

	RESIN
	PRODUCT #
	USES
	Max Temp

	Waxed
	200xx
	Use for general purpose laminating and repair. Contains wax so surface dries non-sticky.  Dries to a amber brown color. Use below the water if gel coated. Heat distortion temp 140F


	140F

	UnWaxed
	201xx
	Use for general purpose laminating and repair. Dries slightly sticky. Dries to a amber brown color. Use below the water if gel coated.

Heat distortion temp 140F


	140F

	Isophthalic
	215xx
	Premium grade resin.  Used for making water tanks. Heat distortion temp 185F.
Can be used in mild acids or alkaline 


	185F

	Vinyl Ester
	217xx
	Used mostly in industry for corrison applications. Resin does not absorb water.  Heat distortion 240F. Vinyl Ester resin has a short shelf life usually less then 60 days. General resin is considered the premium grade.


	240F

	Hetron 197
	225xx
	Hetron 197 has the highest heat distortion temp of any resin 325F continuious.  It can take limited service to 600F.  Excellent resistance to acid.  Comes promoted and has an average shelf life of 90 to 120 days. Easy to fabricate with.


	325F

	Panel Resin
	 230xx
	Use for making translucent laminates, Lamp shades, skylight panels. High UV properties.


	

	Casting Resin
	 240xx
	Cures clear, embed objects , can be machined, can be tinted. Casting up to 2" thick


	 

	Infusion
	219xx
	Low viscosity resin used for infusion has any average gel time 30 min
	140F


